POLISHING TREATMENT OF MERCURY-BEARING LIQUID EFFLUENTS FROM THE CHLOR-ALKALI INDUSTRY BY USING THE BIOMASS SARGASSUM SP

Luis. G. S. Sobral1, André. L. V. Fernandes2, Renata. B. Lima3

1, 2, 3 CETEM – Centre for Mineral Technology (Lsobral@cetem.gov.br)

Abstract: Mercury exhibits high toxicity in any of its occurrence forms in nature. Elemental mercury is highly volatile and can lead to exposure of humans through the inhalation of its vapour or via water or food, when attached to organic structures. One source of mercury emission to the environment is the the mercuric ion (Hg2+)-bearing effluents from the chlor-alkali industry. The main goal of this work is to evaluate the efficiency of the macro-algae Sargassum sp. in natura for ionic mercury uptake, through batch experiments, using a real effluent from a chlor-alkali industry. The results indicate that the macro algae Sargassum sp. in natura is an efficient biosorbent for ionic mercury from effluents of the chlor-alkali industry, reaching 98% removal efficiency  at an initial mercury concentration of 50 ppm. The results obtained in the mercury desorption study showed that mercury is easily removed (elution process) using HCl solution.

# Introduction

The industrial growth and the changes in the production processes have been responsible for an increase in the volume and chemical complexity of discharges to the environment including heavy metal cations. Once released in the environment, some metal cations can accumulate in the food chain, despite being present in low concentrations in the effluent, can accumulate in fishes and animal that are consumed by human beings. In this context, mercury exhibits high toxicity in any of its occurrence forms in nature. Elemental mercury, highly volatile, can lead to man's contamination through the inhalation of its vapour or through water or food, when attached to organic structures. Among the industrial sectors that contribute to mercury contamination of rivers and soils in Brazil and in others nations, one can mention the chlor-alkali industry, which produces chlorine, hydrogen, sodium hydroxide and sodium hypochlorite. There are industrial plants that use the so-called mercury cells, in which the elemental mercury is used as a mobile cathode forming, during the productive process, sodium amalgam. As sources of mercury emission to the environment from this process, one can mention the mercuric ion (Hg2+) bearing effluents [1,2].

In most cases the traditional ways of treating industrial effluents drastically reduces the level of toxic substances. However, the cost associated can be high and the removal efficiency does not always reach a sufficeintly high level. Among the technologies under development, there are many techniques involving microorganisms such as bacteria, fungus and micro-algae[1-8]. The main goal of this work is to evaluate the efficiency of the macro-algae Sargassum sp. in natura for ionic mercury uptake, through batch experiments, using effluents from the chlor-alkali industry.

# Experimental

The macro-algae Sargassum sp. was initially exhaustively washed with de-ionized water to remove solid residues and eliminate the characteristic smell. After that, the biomass was dried in an oven at 60°C for 24h, ground and separated in the particle size range of 0.250 mm to 0.420 mm (35 to 60 mesh) [5]. For accomplishing bio-sorption tests, 100 mL of the effluent was added to a series of 250 mL Erlenmeyer flasks . eMercury was added to each of the solutions to reach initial concentrations of 50, 150, 250, 350, 400 and 450 mg of Hg (II)/L. The pH was 6.0. The contact time was 2h and the concentration of the used biomass was of 2.0 g/L [6]. As the mercury initial concentrations in the effluent were different, the biomass concentration was kept constant, to be able to evaluate the results using the Langmuir and Freundlich isotherm mathematical modeling and determining the adsorptions constants.

The biomass uptake capacity of mercury can be determined from the experimental results obtained at a constant temperature, when the Hg concentration reaches the equilibrium between the liquid and solid phases. The quantity q of Hg uptaken, in this study, expressed in mg of Hg/per gram of biomass, is mathematically expressed by:

q=V(Ci−Cf)M

Where V is the solution volume with initial metal concentration (L), Ci is the initial metal concentration in solution (mg/L), Cf the final, residual or equilibrium metal concentration in solution (mg/L), M the amount of adsorbent (dried biomass) (g) and q the amount of metal removed per solid phase unit (adsorbent) (mg/g). Some desorption experiments were performed to evaluate the kinetics and the possibility of removing the mercury previously adsorbed.

### Results and Discussion

Among the mathematical models commonly used to describe the adsorption characteristics of systems with one component, the Langmuir and Freundlich isotherms deserve a highlight[8]. These models are especially efficient to describe the mercury uptake by Sargassum as this bio-sorbent is inactive, not exhibiting any active mechanisms for mercury uptake [5,8]. After determining the constants of those models, as well as the respective correlation coefficients and some statistical parameters (such as standard deviation and p-level), it is possible to evaluate which model is more appropriate to describe the Hg2+ uptake. In Table 1 the constants values of both mathematical models are shown.

Table 1 - Constant of the mathematical models of Langmuir and Freundlich and their respective correlation coefficients for the Hg (II) biosorption by Sargassum sp.

|  | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| pH | qm (mg/g) | b (L/mg) | R2 | K | 1/n | R2 |
| 6.0 | 82.60  3.73 | 0.096  0.032 | 0.97438 | 22.85  4.95 | 0.234  0.042 | 0.96273 |

In the Langmuir model, the qm constant represents the maximum mercury uptake by Sargassum sp. (expressed as mg of Hg/g of dried biomass) and b is the adsorption energy, which represents the affinity between sorbate and sorbent (expressed in litter of effluent/mg of sorbate). In Figure 1, the Langmuir isotherm is shown.

Figure 1- Profile of the Langmuir isotherm of Sargassum sp. in concentrated effluent (Mercury residual Concentrations: C1 = 3.6 mg/L; C2 = 28.6 mg/L; C3 = 118.0 mg/L; C4 = 191.0 mg/L; C5 = 234.0 mg/L; C6 = 283.0 mg/L; pH = 6.0).

In the obtained Langmuir isotherm, a stabilization region for mercury uptake is evident, which can be related to the hypothesis of the model, according to which the adsorbent material (bio-sorbent) shows a finite number of uptake sites.

In the Freundlich mathematical model, the constant K represents the extension or adsorption capacity of the biosorbent, while the constant 1/n is related to adsorption intensity. In Figure 2 the Freundlich isotherm is presented, obtained using the Quasi-Newton  model for estimating the parameters.

Figure 2 - Profile of the Freundlich isotherm of  Sargassum sp. in concentrated effluent (Mercury residual Concentrations: C1 = 3.6 mg/L; C2 = 28.6 mg/L; C3 = 118.0 mg/L; C4 = 191.0 mg/L; C5 = 234.0 mg/L; C6 = 283.0 mg/L; pH = 6.0)

It is noted that the Freundlich-type curve does not show a region stabilization in mercury uptake, since the Freundlich model does not consider the saturation of uptake sites but rather a mathematically limitless surface.

Conclusions

The results indicate that the macro algae Sargassum sp. in natura is an efficient biosorbent for ionic mercury from effluents from the chlor-alkali industry, reaching 98% removal efficiency  at an initial mercury concentration of 50 ppm. The Langmuir and Freundlich mathematical models describe, efficiently, the ionic mercury uptake within the experimental conditions chosen, which can be shown by the constants values from both models and by the statistical parameters evaluated. As these experimente were conducted at a pH value quite close to the one in chlor-alkali industry effluents (pH = 7.64), it can be concluded that the biosorptive process can be applied in an industrial scale for treating/polishing effluents, and that the reagent costs for controlling the pH can be minimized a great deal. The results obtained in the mercury desorption study showed that mercury is easily removed (elution process) using HCl solution.

References

[1] Fernandes, A. L. V. (2003). Remoção de Mercúrio de Efluentes Líquidos da Indústria Soda-Cloro usando Sargassum sp. Dissertação (Mestrado em Tecnologia de Processos Químicos e Bioquímicos) - Escola de Química / UFRJ, 123p.

[2] FERNANDES, A. L. V.; SOBRAL, L. G. Remoção de mercúrio elementar, de resíduos da Indústria Soda-Cloro, pelo processo de eletrolixiviação. In: V Jornada Interna do CETEM. Rio de Janeiro: 1997. p.91-101.

[3] KAÇAR, Y.; ARPA, Ç.; TAN, S.; DENIZLI, A.; GENÇ, Ö.; ARICA, M. Y. Biosorption of Hg (II) and Cd (II) from aqueous solutions comparison of biosorptive capacity of alginate and immobilized live and heat inactivated Phanerochaete chrysosporium. Process Biochemistry, v. 37, p.601-610, 2002

[4] KAEWSARN, P. Biosorption of copper (II) from aqueous solutions by pre-treated biomass of marine algae Padina sp. Chemosphere, v.47, p.1081-1085, 2002.

[5] KRATOCHVIL, D.; VOLESKY, B. Advances in the biosorption of heavy metals. TIBTECH, v.16, p.291-300, 1998.

[6] SAGLAM, A.; YALÇINAKAYA, Y.; DENIZLI, A. et al.. Biosorption of mercury by carboxymethylcellulose and immobilized Phanerochaete chrysosporium. Microchemical Journal, v.71, p.73-81, 2002.

[7] VALDMAN, E. Uso de Sargassum sp. Residual como biossorvente para cádmio, cobre e zinco. 2000. 146p.  Dissertação (Mestrado em Tecnologia de Processos Químicos e Bioquímicos) - Escola de Química, Universidade Federal do Rio de Janeiro, Rio de Janeiro.

[8] VOLESKY, B.; HOLAN, Z. R. Biosorption of heavy metals. Biotechnology Progress, v.11, p.235-250, 1995.