Biosorption of Mercury by Rice Husk

Uzaira Rafique*., Sumreen Iqbal., and Uzma Rafique.

Environmental Sciences Program

Fatima Jinnah Women University, The Mall Rawalpindi., Pakistan 46000

uzairaiqbal@yahoo.com

Abstract

Vegetation waste can remove toxic heavy metals by adsorption, chelation and ion exchange, thus can be exploited for environmental pollution control. In the present study rice husk (a non-conventional waste material) was used to determine the removal efficiency of mercury. Rice husk was washed with distilled water, dried in oven and grinded. Mercuric chloride from BDH (99.5%) was used to prepare standard mercury solutions  of different strengths (i.e. 0.2ppm -8ppm). One gram of the grinded waste (rice husk) was soaked in 25 ml mercury solution of different strengths of variable period of time with an interval of 15 minutes up to 120 minutes. The supernatant (3ml) of each decant solution was run on U.V-visible Spectrophotometer (UV-1601, Shimadzu) at 492 nm, to determine the remained metal concentration. Maximum adsorption capacity was found for 0.6, 4, 5 and 6 ppm standard mercury solutions after 120 minutes, depicting the highest efficiency (95%) of the waste. A gradual decrease in pH of the soaked waste solution was found with time. Biosorption coefficient (q) was also calculated from Freundlich and Langmuir Model.

Keywords:

- Rice Husk, Biosorption Coefficient, Heavy Metals

# Introduction

Industrial processes produce huge amounts of wastewater daily, which are usually discharged untreated into the surrounding environment, leading to detrimental chemical, thermal, and biological effects on aquatic, plant and human life. Conventional methods for removing the dissolved heavy metal ions include chemical precipitation, chemical oxidation and reduction, ion exchange, filtration, electrochemical treatment and evaporative recovery. In addition, the parametric pumping with pH changing, filtration using reverse osmosis, nano-filtration, and ultra-filtration are enhanced with complexation (Holl , 2001 and Neyenset.al., 2001).

Biosorption has been proposed as a potential alternative for removing toxic heavy metals. Important physical and chemical parameters, for effectively decontaminating the metal contaminated waters, using environmental friendly biomass, are studied. Biosorption by non-living biomasses has been found particularly effective in binding heavy metal ions. High sorption capacity, easy regeneration and low costs make biomass of special interest for the purification of high volumes of low-heavy metals concentration wastewater (Hutton et.al., 1986), which is either difficult and/or expensive to accomplish by conventional metal-removal processes.

Vegetation wastes are being studied to develop a decontamination method that is efficient, safe and environmentally friendly. Fibrous natural ion exchangers are likely to be a viable alternative to the polymeric chelating exchanger. They provide their durability, morphology and heavy metal selectivity (Neyens et.al., 2001). It is particularly the cell wall structure of certain vegetation, which is found responsible for this phenomenon.  Vegetation wastes include ligninocellulosic materials such as agricultural residues and other plant substances. Lignocellulosic materials are characterized by high degree of diversity and variability in their properties. All organic exchangers used in waste management have a synthetic polymer backbone containing cellulose, hemicellulose and lignin (Reed et.al., 1994) for which they have the potential to act as ion exchangers. Vegetation wastes have been proved suitable for being used as heavy metal sorbent (Delgado et.al., 1998).

## Experimental

Vegetation waste (Rice Husk) was used to remove mercury from the aqueous solutions. Rice husk was washed with distilled water three to four times to remove particulate material from the surface, further oven-dried at 80ºC for 24 hours. After drying the waste was grinded to attain a uniform smaller particle size. Analytical grade HgCl2 was dissolved in distilled water in order to obtain a solution containing mercury at the concentrations from 0.6 to 8 ppm. 25 ml of each standard solution was added to 1 gram of vegetation waste and the removal efficiency was observed after every 15 minutes. The solution was sampled and analyzed for metal concentration by U.V-visible Spectrophotometer, model UV-1601, Shimadzu Japan, using dithiazone as complexing agent.

Results and Discussion

A number of different metal-binding mechanisms has been suggested as being active in biosorption such as chemisorption by ion exchange, complexation, coordination, chelation; physical adsorption, micro precipitation. The biomass of rice husk demonstrated a good capacity of mercury biosorption, revealing its potential for effluent treatment. Maximum adsorption capacity was found for 0.6, 4, 5 and 6 ppm standard mercury solutions after 120 minutes, depicting the highest waste efficiencies, which was nearly 95%. A gradual decrease in pH of the soaked waste solution was detected with time.

Figure 1- Variation of mercury concentration with time from different  initial mercury concentrations  ( 0.6 to 3 ppm)                                                                                                 Figure 2- Variation of mercury concentration with time from different  initial mercury concentrations  ( 4 to 8 ppm)

The mercury biosorption coefficient (q), for raising the sorption isotherms was calculated from the initial concentration (Ci) and the final or equilibrium concentration (Cf) in every flask, as follows:

q = V(Ci-Cf)

### M

where, V is the volume of the mercury solution in the flask and M is the dried mass of biosorbent. Two models were used to fit the experimental data: the Langmuir model and the Freundlich model. The Langmuir sorption model was chosen for estimating the maximum metal biosorption by the biosorbent. The Langmuir isotherm can be expressed as:

q=qmaxbCf(1+bCf)

where b is a constant related to the adsorption/desorption energy, and qmax is the maximum biosorption after completely saturating the surface.  Linear plots between the log (q) and log (Cf) showed that the adsorption obeys the Langmuir and Freundlich isotherm models. The maximum values of qmax and biosorption coefficients were found for 0.6, 4, 5 and 6 ppm mercury solution at maximum time of 120 minutes.

Figure 3 plot of Log Cf and Log q for 5 ppm mercury solution                                                                               Figure 4 plot of Log Cf and Log q for 6 ppm mercury solution

Figure 4  plot of Log Cf and Log q for 5 ppm mercury solution

Figure 5 plot of Log Cf and Log q for 5 ppm mercury solution

The biomass materials offer numerous molecular groups which are known to offer ion exchange sites. The carboxyl, sulfate, phosphate, amine, phenolic and hydroxylic could be the main ones to which exchange properties of these wastes are attributed and these wastes can be exploited for environmental pollution control (Eneida et.al., 2002).   The mercury Biosorption by rice husk is found minimum during the first 15 minutes and increasing its  efficiency toward the end of the experiments and at low pH . It is well established that heavy metals are taken up from water predominantly by ion exchange. An increase in the pH is detected within the first hour of the experiments and then started to decrease, which may be the result of dissolution of some components of the rice husk. It may be due to the fact that organic materials sorb cations with concurrent release of equivalent number of other cations (Holan et.al., 1993). More recent studies with biomass have indicated a dominant role of ion exchange metal binding.

# Conclusion

Biosorption is a property of certain types of inactive, or dead biomass, to bind and concentrate heavy metals from very dilute aqueous solutions. Biomass exhibits this property, acting just as a chemical substance, as an ion exchanger of biological origin. The vegetation wastes have been shown to be effective in sorption of heavy metal ions. Rice husk have shown a potential to act as biosorbent. The study concluded that the rice husk can adsorb a sufficient amount of mercury from synthetic mercury solution and can be used to effluent treatment processes. The effect of pH and time is significant. The increase in time and decrease in pH can enhance the adsorbing properties of that biomass.

References

Hutton, M.; Symon, C. (1986) Quantities of cadmium, lead, mercury and arsenic entering the environment from human activities. Sci. Total. Environ., 57, 129-150,.

HÖll, W.H. (2001).Separation of mixtures of heavy metals by parametric pumping with variation of pH, 6th World Congress of Chemical Engineering, Melbourne, Australia

Neyens, E.; Juliastuti, S.R.; Hulpiau, H. (2001).Reverse osmosis, nanofilteration and enhanced ultrafilteration of wastewaters, 6th World Congress of Chemical Engineering, Melbourne, Australia 23-27 September, 2001

Reed, B.E.; Arunachalam, S.; Thomas, B. (1994). Removal of lead and cadmium from aqueous waste streams using granular activated carbon columns, Environmental Progress, Vol.13, 60-64.

Delgado, A.; Anselmo, A.M.; Novals, J.M., (1998).Heavy metal biosorption by dried powdered mycelium of fusarium flocciferum., Water Environmental Research, 70, 370-375,

Holan, Z.R.; Voleskey, B. and Prasetyo, I. (1993) Biosorption of cadmium by biomass of marine algae. Biotechnology and Bioengineering, , vol. 41, p. 819- 825.

Eneida S.C., Celia R.G.T., Teresa M. K.R., , (2002), Biosorption of Chromium (III) by Sargassum Sp. Biomass. Electronic Jounrnal of Biotechnology, Vol 5(2)