Mercury Removal from Exhausted Fluorescent Lamps: I) The ultimate Oxidative Processes

L. G. S. Sobral* (Lsobral@cetem.gov.br) , R. L. C. Santos* (rsantos@cetem.gov.br) , B. R. S. Costa* (byron@cetem.gov.br) , F. J. V. Paiva* (fpaiva@cetem.gov.br)

*CETEM – Centro de Tecnologia Mineral – Av. Ipê 900, Ilha da Cidade Universitária, Rio de Janeiro, RJ, Brasil, Cep: 21941-590, http://www.cetem.gov.br

Abstract - In this technical contribution, oxidative processes were considered for treating the inner white coating of the lamps (mainly fluorchlorapatite - Ca5(PO4)3(F,Cl)), the major source of mercury in order to establish a comparison in terms of mercury removal efficiency and energy savings. Among those processes, the eletroleaching and the chemical treatments, more specifically the use of strong oxidants such hypochlorite and nitric acid solutions were tested, without disregarding the possibility of recycling the aforementioned compound back to the fluorescent lamp production. The results obtained so far show that the processes used are quite efficient in terms of mercury removal, (>99%). The electroleaching yielded better results taking into consideration that the mercury is recovered as elemental mercury, whereas the chemical methods produce mercury as soluble species which needs further processing.

Introduction

Energy efficient fluorescent lamps have gained widespread usage over the years in comparison to incandescent one. This increasing use of mercury containing fluorescent lamps have led to growing concerns over their proper disposal.

Nowadays the primary fate of mercury-containing lamps is to be disposed of as common trash. Public and industrial sectors are the biggest generators of fluorescent lamp disposal (HID – high intensity discharge). We verified that companies and public departments, in general, are not aware of adverse effects caused by mercury and since there is no specific legislation, they do not know how to deal with such waste. In 1998, 48.5 millions mercury lamps were discarded in Brazil, which represents a Hg amount of 1000 kg (20.6 mg per lamp).

Depending on the type of lamp and of the technology used in its production, a fluorescent lamp can have from 10 to 300 mg of mercury [1]. In most lamps these values oscillate between 60 and 120 mg[2], with 80mg as an average value for fluorescent lamp[3]. Even low power lamps, like for instance, fluorescent lamps of just 40W, have about 10 mg of mercury[4,5].

In 2000, the total amount discarded was 80 millions and this number will be growing with Brazilian program of energy conservation. The focus of this potential contamination is located in the Southeast region, where 60% of Brazilian economy is generated. Of the total number of lamps disposed in this region, only 3% have environmentally friendly disposal by means of recycling. This disposal was carried out voluntarily by companies that have a disposal-controlled system for their waste and/or by those interested in being certified by ISO 14.000.

In this technical contribution, oxidative processes were considered for treating the inner white coating of the lamps (fluorchlorapatite - Ca5(PO4)3(F,Cl), as the main compound), the major source of mercury in order to establish a comparison in terms of mercury removal efficiency and energy savings. Among those processes, eletroleaching and chemical treatments, more specifically the use of strong oxidants such hypochlorite and nitric acid solutions were used, without disregarding the possibility of recycling the aforementioned compound back to the fluorescent lamp production.

The results obtained so far show that the processes used are quite efficient in terms of mercury removal, which are higher than 99%. However, the electroleaching presented better results taking into consideration that the mercury is recovered as elemental mercury, whereas the chemical methods that yields mercury as soluble species need further processing to get there.

Experimental

The electroleaching tests were accomplished in a reaction system depicted in Figure 1 [1], which was composed of a 250 mL beaker with two graphite electrodes (anode and cathode) in, and the white powder (Ca5(PO4)3(F,Cl)) being mechanically suspended in a 1M NaCl solution. The chemical reaction tests, using the two different oxidizing agents (HNO3 and NaClO), were carried out by mechanically suspending the white powder in such solutions for a specific period of time.

Fig. 1- Reaction system for the electroleaching tests.

Results and Discussion

As can be observed in Table 1, the mercury removal efficiency was very high as the elemental mercury, apart from being very low in content, was completely available to be oxidised by the oxidant species generated in the bulk solution, as shown in the following reactions: (Cl2+H2OÛHClO+H++Cl−) and (HClOÛClO−+H+); the concentration of HClO and ClO- will depend upon the pH of the solution. Those species are generated as a result of the chemical reaction of the chlorine, being released at the anode surface due to the chloride ions oxidation (2Cl−ÛCl2+2e), in the aqueous phase. In addition, at pH 4 the results were even better since the possibility of producing calomel (Hg2Cl2) decreases dramatically at this pH. Should calomel, a quite insoluble mercury compound, be formed it would remain in the white powder which would compromise the final quality of it.

Table 1- Results of mercury extraction by electroleaching.

| White Powder at pH:1 |  |  | White Powder at pH:4 |  |  |
| --- | --- | --- | --- | --- | --- |
| Extraction | [Hg] (%) | Efficiency | Extraction | [Hg] (%) | Efficiency |
| 0 | 0.23 % | - | 0 | 0.23 % | - |
| 1 | 40 ppm | 81.8 % | 1 | 27.6 ppm | 88.5 % |
| 2 | 4.6 ppm | 98,1 % | 2 | 2.3 ppm | 99.5 % |

The tests with nitric acid were found to be quite effective for dissolving the mercury, but it was realised that apart from dissolving the elemental mercury, it was aggressive enough to dissolving the white powder, which was not the aim of this technical contribution. The initial idea was to return both, the mercury and the white powder, back to the fluorescent lamp production process.

In the case of the use hypochlorite the results show a quite clear trends in terms of the experimental parameters, such as: temperature, hypochlorite concentration and leaching time. In Table 2, the experimental conditions for the mercury removal tests are shown, while Figure 2, shows the efficiency of the mercury extraction, taking into consideration the interaction among those parameters.

Table 2 – Parameters and outline conditions for the mercury removal tests.ção de mercúrio

| Parameters | Level 1 | level 2 |
| --- | --- | --- |
| Temperature (ºC) | 25 | 50 |
| Leaching Time ( min) | 30 | 60 |
| [NaClO] (%) | 7%(m/m) | 14%(m/m) |

Fig. 2- Influence of some experimental parameters on the mercury recovery.

From the experimental results, we can infer that the temperature and the hypochlorite concentration are independent parameters. From the graphs 1, 2 and 3 one can verify that the mercury removal efficiency from the fluorchlorapatite is most efficient when all of the parameters (temperature, leaching time and hypochlorite concentration) are in their highest levels.

Once the highest level for the hypochlorite concentration is equal to the concentration limit of this reagent, the optimization of mercury removal will be focused on the highest temperature and leaching time.

Conclusions

Taking into consideration the results obtained so far, one can conclude that:

The nitric acid is quite effective in dissolving mercury, but the main goal was not reached, which was to return both the mercury and white powder back to fluorescent lamps production;

The use of hypochlorite was effective in removing mercury with well defined experimental conditions, although one has to bear in mind that after leaching the mercury it is necessary to extracting the mercury from the aqueous phase, either by electrolysis it or cementing it with metallic aluminium;

Regarding the electrolytical process, these tests suggest it is the most effective since it is quite feasible to remove the elemental mercury in a one step process.

References

[1] E.P. Yanin e N.N. Moskalenko – Monitoring and Assessment of Mercury Pollution Fedorov VV 1992 – Luminescent Lamps - Energoatomizdat, Moscow (in Russian).

[2] Kokinov  AM, Fedorenko AS, Prytkov AA 1994 – Methods for Mercury Hazard Reduction in Production and Use of Light Sources. In: Mercury Hazards – The Problem of the 20th Century. The Foundation for Mercury Hazards, St. Petersburg, pp 79-82 (in Russian)

[3] Avrukh V.S. 1994 – Waste Mercury-Containing Lamps are an Environmental Hazard. In: Mercury Hazards – The Problem of 20th Century. The Foundation for Mercury Hazards, St. Petersburg, pp 38-44 (in Russian)

[4] Ohbayashi, H., Saitoh, S., Melber, A. – Removal of Mercury from Fluorescent Lamps by Vacuum Thermal Recycling – Env. Res. Laboratory, Z.E.R.O., JAPAN Co., Japão; ALD Vacuum Technologies AG, Alemanha

[5] Waymaus J.F. 1987 – The State and Perspectives of Discharge Light Sources – Svetoteknika 5:20-24 (in Russian) (26-31)

[6] L. G. S. Sobral et. al., Electroleaching Process for Remediation of Mercury Contaminated Soils, Contaminated Soil’95, vol. II, pag. 1337-1347, proceedings of the International FZK/TNO Conference on Contaminated Soil, 30 October – 3 November, 1995, Maastricht, Netherlands.