Efficiency of Industrial Minerals on the Removal of Mercury Species from Liquid Effluents

Ricardo Melamed and Adão Benvindo da Luz

CETEM/MCT – Center for Mineral Technology

Av. Ipê 900, Ilha da Cidade Universitária, 21941-590, Rio de Janeiro, Brazil

RMELAMED@cetem.gov.br

## Abstract

Increasing attention by the industrial sector has been given to the removal of mercury from liquid effluents to fulfill the environmental regulations. The processes usually utilized include chemical precipitation, cementation, ion exchange, adsorption and solvent extraction. All these methods have limitations such as slow kinetics, low adsorption capacity and they are usually very expensive. Thus, new technologies for mercury removal are of great interest. In this regard, the use of industrial minerals for the removal of heavy metals in general has been studied.

This study had the goal to test the efficiency of many industrial minerals to remove mercury from liquid effluents. The methodology involved a batch adsorption technique. The tested minerals included: atapulgites, zeolites, magnetites, kaolin, vermiculite and bentonite.

Preliminary results show considerable efficiency by magnetite and zeolite on mercury removal. These minerals were capable to remove mercury species from effluents with concentrations reaching 1,000 ppm, corresponding to a sorption capacity of 10,000 mg Hg/kg. The maximum sorption was not reached in these preliminary tests. In addition, it became evident the importance of mercury speciation at the solid:liquid interface, with consequences on the application of this technology to effluent treatment.

Key words: adsorption, speciation, effluent treatment, mineral characterization

Introduction

Mercury is a highly toxic heavy metal, which is still used in various anthropogenic activities such as the chlor-alkaly industry, fluorescent lamps and in the recovery of gold. It is naturally present in various concentrations in coal, natural gas and petroleum. Once delivered to the environment, the behavior of Hg is very complex because it may be present in different oxidation states with different physico-chemical properties.

To satisfy environmental regulations, towards the removal of heavy metals from liquid effluents, the industrial sector has been employing processes such as precipitation, cementation, ion exchange, solvent extraction and adsorption. Limitations of these methods are: slow kinetics, low adsorption capacity and high cost. Thus, the use of industrial minerals with low cost and high sorption capacities has been tested for removing heavy metals in general. Data on the use of these minerals for mercury removal is scarce.

This study aimed at verifying the efficiencies of different industrial minerals in the removal of Hg species from liquid effluents.

Experimental

A batch adsorption technique was conducted in centrifuge tubes containing 4g of various minerals and 40 mL of solution containing increasing concentrations of Hg, from 10 ppb to 10 ppm in different electrolytic systems: 0.1 M  NaCl or NaNO3.

The minerals studied were: Atapulgite, Bentonite Bahia, Bentonite Paraíba, Caulim Magnetite, Vermiculite, Zeolite.

After reacting for 48 hours in a shaker, tubes were centrifuge for 20 minutes at 3500 rpm and filtered through 0.45 μm paper. Both phases were preserved for further analysis.

The most promising materials were submitted to the same tests but with initial Hg concentrations varying from 750 to 1000 ppm.

In addition, desorption studies from the most efficient materials were also conducted in the same units that were used for adsorption tests with 100 ppm of Hg. The desorption tests were conducted in the same electrolyte system that were used for adsorption tests and, in addition, we utilized acids with the same ligands and ionic strengths.

The analytical chemistry for Hg employed the cold vapor atomic absorption spectrometer.

Results and Discussion

The adsorption efficiency of each mineral was calculated in percentage of the initial concentration, and the results are shown in Table 1.

Table 1. Mercury percentage retained by the industrial minerals in two electrolyte systems with Ionic Strength of 0.1 M.

|  | Effluent Concentration |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Minerals | 10 ppb |  | 100 ppb |  | 1 ppm |  | 10 ppm |  |
|  | NaCl | NaNO3 | NaCl | NaNO3 | NaCl | NaNO3 | NaCl | NaNO3 |
| Atapulgite | 100 | 100 | 100 | 100 | 100 | 100 | 74 | 100 |
| Bentonite Bahia | 100 | 100 | 100 | 95 | 0 | 78 | 0 | 41 |
| Bentonite Paraíba | 100 | 100 | 100 | 100 | 59 | 96 | 44 | 60 |
| Caulim | 100 | 100 | 61 | 99 | 0 | 92 | 0 | 67 |
| Magnetite | 99 | 99 | 100 | 100 | 100 | 100 | 100 | 100 |
| Vermiculite | 100 | 100 | 100 | 100 | 100 | 100 | 99 | 100 |
| Zeolite | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 |

Table 1 shows that the industrial minerals magnetite, vermiculite and zeolite had higher removal efficiencies than the other ones, for Hg concentrations up to 10 ppm in both electrolyte systems. To these 3 minerals retention tests were imposed with Hg concentrations up to 1000 ppm. Results are presented in Table 2.

Table 2. Hg percentage removed by industrial minerals in two electrolyte systems at 0.1 M Ionic Strength.

|  | Effluent Concentration |  |  |  |
| --- | --- | --- | --- | --- |
| Minerals | 750 ppm |  | 1000 ppm |  |
|  | NaCl | NaNO3 | NaCl | NaNO3 |
| Magnetite | 99 | 100 | 99 | 99 |
| Vermiculite | 47 | 76 | 45 | 67 |
| Zeolite | 92 | 98 | 97 | 99 |

Results in Table 2 indicate that both magnetite and zeolite kept their high efficiencies on Hg species removal even for initial concentrations of 1000 ppm, while the efficiency of vermiculite declined.

Results in Table 3 show that higher desorption and recovery of Hg were achieved from vermiculite than from the magnetite, which infer the different mechanisms in the retention of Hg by these minerals.

Table 3. Desorption of Hg from magnetite and vermiculite after retention of 100% of 100 ppm Hg.

| Minerals | % Desorption |  |  |  |
| --- | --- | --- | --- | --- |
|  | NaCl | NaNO3 | HCl | HNO3 |
| magnetite | 0 | 0 | 0 | 0.5 |
| vermiculite | 3.3 | 0.05 | 49.6 | 34.3 |

Results shown in Tables 1, 2 and 3 also indicate the importance of Hg speciation in the retention process by the minerals. In this regard we point out that, in the NaCl system, the prevaling species is HgCl42-, which have a lower interaction at the solid:liquid interface of those minerals than species such as Hg(H2O)5OH+ produced in the NaNO3 system.

# Bibliography

Fitzgerald WF, Engstrom DR., Mason Rp, Nater. (1998). The case of atmospheric mercury contamination in remote areas.  Eviron. Sci. Technol. 32/1:1-7.

Gavis L, Ferguson J. (1972). The cycling of mercury though the environment, Water res. 6:989-1008.

H.Biester G. Muller, H.F.Scholer. (2002) Estimating distribution and retention of mercury in three different soil contaminated by emissions from chlor-alkali plants: part I. The Science of the Total Enviroment 284:177-189

J. Barron-Zambrano, S.Laborie, Ph. Vier, M.Rakib, G. Durand (2002) Mercury removal fromaqueous solutions by complexation-ultrafiltration. Desalination 144:201-206